Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 10 21 13 - TOILET COMPARTMENTS

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section Includes:

Stainless-steel toilet compartments configured as [toilet enclosures] [entrance screens] [and] [urinal screens].

Phenolic-core toilet compartments configured as [toilet enclosures] [entrance screens] [and] [urinal screens].

Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

Steel overhead support is generally required for ceiling-hung units; wood construction does not provide adequate support.

Section 05 50 00 "Metal Fabrications" for supports that attach [ceiling-hung compartments] [floor-and-ceiling-anchored compartments] [and] [post-to-ceiling screens] to overhead structural system.

Wood may provide adequate overhead support for floor-and-ceiling-anchored compartments and post-to-ceiling screens but is inadequate for supporting ceiling-hung compartments.  Consult manufacturers for recommendations.

[Section 06 10 00 "Rough Carpentry"] [Section 06 10 35 "Miscellaneous Rough Carpentry"] for [blocking] [overhead support of floor-and-ceiling-anchored compartments] [and] [overhead support of post-to-ceiling screens].

Retain subparagraph below unless accessories are inserted in this Section.  Some manufacturers offer a limited number of standard accessory items.  Verify availability with manufacturers selected.

Section 10 28 00 "Toilet, Bath, and Laundry Accessories" for toilet tissue dispensers, grab bars, purse shelves, and similar accessories.

ACTION SUBMITTALS

Product Data:  For each type of product indicated.  Include construction details, material descriptions, dimensions of individual components and profiles, and finishes.

LEED Submittals (Projects authorized for LEED certification only)

"Product Data for Credit IEQ 4.4" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS.

Product Data for Credit IEQ 4.4:  For particleboard, documentation indicating that product contains no urea formaldehyde.

"Laboratory Test Reports for Credit IEQ 4" Subparagraph below applies to LEED for Schools.

Laboratory Test Reports for Credit IEQ 4:  For [adhesives] [and] [composite wood products], documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

Shop Drawings:  For toilet compartments.  Include plans, elevations, sections, details, and attachments to other work.

Retain first subparagraph below if required or revise to suit Project.

Show locations of cutouts for compartment-mounted toilet accessories.

Retain first subparagraph below if required for metal units; see "Metal Units, General" Article in the Evaluations.

Show locations of reinforcements for compartment-mounted grab bars.

Show locations of centerlines of toilet fixtures.

Show[ ceiling grid and] overhead support or bracing locations.

Samples for Initial Selection:  For each type of unit indicated.  Include Samples of hardware and accessories involving material and color selection.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain paragraph below with or without above.

Samples for Verification:  For the following products, in manufacturer's standard sizes unless otherwise indicated:

Each type of material, color, and finish required for units, prepared on 6-inch- (152-mm-) square Samples of same thickness and material indicated for Work.

Each type of hardware and accessory.

INFORMATIONAL SUBMITTALS

Retain paragraph below for product certificates from manufacturers.

Product Certificates:  For each type of toilet compartment, from manufacturer.

CLOSEOUT SUBMITTALS

Maintenance Data:  For toilet compartments to include in maintenance manuals.

QUALITY ASSURANCE

Consider retaining first paragraph below for Federal projects.

Comply with requirements in GSA's CID-A-A-60003, "Partitions, Toilets, Complete."

Retain first paragraph below if Owner or authorities having jurisdiction require that toilet compartments made of combustible materials comply with surface-burning requirements.  Metal units are inherently noncombustible.  Flame-spread index options correspond to flame-spread and smoke-developed Classes A, B, and C; verify, with manufacturers selected, availability of suitable units.  See "Fire-Test-Response Characteristics" Article in the Evaluations.

Surface-Burning Characteristics:  As determined by testing identical products according to ASTM E 84, or another standard acceptable to authorities having jurisdiction, by a qualified testing agency.  Identify products with appropriate markings of applicable testing agency.

Flame-Spread Index:  [25] [75] [200] or less.

Smoke-Developed Index:  450 or less.

Regulatory Requirements:  Comply with applicable provisions in [the U.S. Architectural & Transportation Barriers Compliance Board's "Americans with Disabilities Act (ADA) and Architectural Barriers Act (ABA) Accessibility Guidelines for Buildings and Facilities"] [and] [ICC/ANSI A117.1] for toilet compartments designated as accessible.

PROJECT CONDITIONS

Field Measurements:  Verify actual locations of toilet fixtures, walls, columns, ceilings, and other construction contiguous with toilet compartments by field measurements before fabrication.

Insert article for warranty requirements if required.  Availability varies among manufacturers and by type of unit.  When special warranties are required, verify with Owner's counsel that special warranties are not less than remedies available to Owner under prevailing local laws.

PRODUCTS

MATERIALS

In this article, retain only materials that are referenced in other articles under specific units and accessories required.

Aluminum Castings:  ASTM B 26/B 26M.

Aluminum Extrusions:  ASTM B 221 (ASTM B 221M).

Brass Castings:  ASTM B 584.

Brass Extrusions:  ASTM B 455.

first two paragraphs below for stainless-steel brackets (fittings).  Manufacturers make brackets (fittings) from either material and often do not state which is used.

Stainless-Steel Sheet:  ASTM A 666, Type 304, stretcher-leveled standard of flatness.

Stainless-Steel Castings:  ASTM A 743/A 743M.

Insert specific zamac-alloy number in first paragraph below if required.  Zamac alloys are termed "traditional" in ASTM B 86 and have a range of mechanical properties.  Some manufacturers designate particular zamac-alloy numbers in their specifications.

Zamac:  ASTM B 86, commercial zinc-alloy die castings.

Retain second option in "Particleboard" Paragraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.4.  Retain third option if required for LEED for Schools Credit IEQ 4.

Retain "Adhesives" Paragraph below if required for LEED for Schools Credit IEQ 4.

Adhesives:  Manufacturer's standard product that complies with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

STAINLESS-STEEL UNITS <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two paragraphs and list of manufacturers below.  See Section 016000 "Product Requirements."

Manufacturers:  Subject to compliance with requirements, provide products by one of the following :

Basis-of-Design Product:  Subject to compliance with requirements, provide  General Partitions; 40 Series; General Partitions Mfg. Corp.; www.generalpartitions.com or comparable product by one of the following:

Bradley Corporation; Mills Partitions; Series 400 Sentinel; www.bradleycorp.com.

Global Steel Products Corp; www.globalpartitions.com.

Substitutions:  See Section 01 25 00 - Substitution Procedures.

Retain first three paragraphs below to suit Project.

Toilet-Enclosure Style:  Floor anchored/Overhead braced   .

Urinal-Screen Style:      Floor anchored/Overhead braced .

Some manufacturers weld face sheets together at corners; others do not.  Revise first paragraph below to suit Project.  Before retaining option, verify availability with manufacturers selected.  See Evaluations.

Door, Panel, and Pilaster Construction:  Seamless, metal facing sheets pressure laminated to core material; with continuous, interlocking molding strip or lapped-and-formed edge closures; corners secured by welding or clips and exposed welds ground smooth. Exposed surfaces shall be free of pitting, seam marks, roller marks, stains, discolorations, telegraphing of core material, or other imperfections.

Revise subparagraphs below to suit Project.  See Evaluations.

Core Material:  Manufacturer's standard sound-deadening honeycomb of resin-impregnated kraft paper in thickness required to provide finished thickness of 1 inch (25 mm) for doors and panels and 1-1/4 inches (32 mm) for pilasters.

Grab-Bar Reinforcement:  Provide concealed internal reinforcement for grab bars mounted on units.

If necessary, insert requirements for internal reinforcement where small compartment-mounted accessories, such as toilet tissue dispensers, are attached; see "Metal Units, General" Article in the Evaluations.

Tapping Reinforcement:  Provide concealed reinforcement for tapping (threading) at locations where machine screws are used for attaching items to units.

Urinal-Screen Construction:

Retain one or more of three subparagraphs below; if retaining more than one, indicate locations of each type on Drawings or by inserts.  Retain second subparagraph for government-style metal screens; coordinate with manufacturers selected.

Flat-Panel Urinal Screen:  Matching panel construction.

Facing Sheets and Closures:  Stainless-steel sheet of nominal thicknesses as follows:

Before revising seven subparagraphs below, see "Metal Units, General" Article, and its accompanying table, in the Evaluations for discussion of steel sheet thicknesses; the table correlates traditional gage numbers with specified decimal thicknesses.

Pilasters, Braced at Both Ends:  Manufacturer's standard thickness, but not less than 0.038 inch (0.95 mm).

Retain subparagraph above for overhead-braced and floor-and-ceiling-anchored mounting styles.  Retain first subparagraph below for floor-anchored and ceiling-hung mounting styles.

Retain first option in first subparagraph below to maximize competition among listed manufacturers.  Second option will eliminate some manufacturers or require custom fabrications.

Panels:  Manufacturer's standard thickness, but not less than 0.031 inch (0.79 mm) [0.038 inch (0.95 mm)].

Doors:  Manufacturer's standard thickness, but not less than 0.031 inch (0.79 mm).

Retain one of three subparagraphs below if required.  Retain second subparagraph for government-style metal screens; coordinate with manufacturers selected.

Flat-Panel Urinal Screens:  Thickness matching the panels.

Pilaster Shoes  :  Stainless-steel sheet, not less than 0.031-inch (0.79-mm) nominal thickness and 3 inches (76 mm) high, finished to match hardware.

Retain first paragraph below for floor-anchored, overhead-braced, and post-to-ceiling urinal screens.

Urinal-Screen Post:  Manufacturer's standard post design of material matching the thickness and construction of pilasters   ; with shoe matching that on the pilaster.

Brackets (Fittings):

Retain one or both subparagraphs below; if retaining both, indicate locations of each type of fitting on Drawings or by inserts.  If necessary, revise to indicate fitting requirements for specific applications, e.g., "heavy-duty" urinal-screen brackets.  See Evaluations.

Full-Height (Continuous) Type:  Manufacturer's standard design; stainless steel .

Textured finishes are available from some manufacturers, but textures vary.

Stainless-Steel Finish:   Manufacturer's standard textured finish Leather on exposed faces.  Protect exposed surfaces from damage by application of strippable, temporary protective covering before shipment.

PHENOLIC-CORE UNITS <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two paragraphs and list of manufacturers below.  See Section 016000 "Product Requirements."

Manufacturers:  Subject to compliance with requirements, provide products by one of the following :

Basis-of-Design Product:  Subject to compliance with requirements, provide  General Partitions; 40 Series; General Partitions Mfg. Corp.; www.generalpartitions.com or comparable product by one of the following:

Bobrick Washroom Equipment, Inc; 1082.67; www.bobrick.com.

Global Steel Products Corp; www.globalpartitions.com.

Substitutions:  See Section 01 25 00 - Substitution Procedures.

Retain first three paragraphs below to suit Project.

Toilet-Enclosure Style:  Floor anchored/Overhead braced   .

Urinal-Screen Style:  Floor anchored/ Overhead braced] .

Before retaining option in first paragraph below, verify availability with manufacturers selected.  See Evaluations.

Door, Panel, and Pilaster Construction:  Solid phenolic-core panel material with melamine facing on both sides fused to substrate during panel manufacture (not separately laminated), and with eased and polished edges.  Provide minimum 3/4-inch- (19-mm-) thick doors and pilasters and minimum 1/2-inch- (13-mm-) thick panels.

Pilaster Shoes  :  Fabricated from stainless-steel sheet, not less than 0.031-inch (0.79-mm) nominal thickness and 3 inches (76 mm) high, finished to match hardware.

Retain first paragraph below for floor-anchored, overhead-braced, and post-to-ceiling urinal screens.  First option is sometimes used with floor-mounted, phenolic-core urinal screens; verify, with manufacturers selected, availability and cut-out design.

Urinal-Screen Post:  Manufacturer's standard post design of  material matching the thickness and construction of pilasters   ; with shoe matching that on the pilaster.

Brackets (Fittings):

Retain one or both subparagraphs below; if retaining both, indicate locations of each type of fitting on Drawings or by inserts.  If necessary, revise to indicate fitting requirements for specific applications, e.g., "heavy-duty" urinal-screen brackets.  See Evaluations.

Full-Height (Continuous) Type:  Manufacturer's standard design; stainless steel .

Phenolic-Panel Finish:

Facing Sheet Finish:  [One color and pattern] [Two colors and patterns] in each room.

Solid "through-color" phenolic panels described by second option in subparagraph below are available from Global and, perhaps, from other manufacturers; verify availability with manufacturers selected.

Color and Pattern:   As selected by Architect from manufacturer's full range color to be determined, with manufacturer's standard dark color core .

ACCESSORIES

Before revising first paragraph below, verify requirements of authorities having jurisdiction for accessible toilet facilities.

Hardware and Accessories:  Manufacturer's standard design, heavy-duty operating hardware and accessories.

Retain six subparagraphs below or revise to suit Project.

Material:    Stainless steel .

Hinge types vary in availability among manufacturers; most offer paired hinges listed below.  Paired hinges can be either preset or adjustable; for preset, insert requirements in first subparagraph below for hold-open angle.  Retain last option only if retaining solid-polymer doors and pilasters configured to receive integral hinges.

Hinges:  Manufacturer's standard  continuous, cam type that swings to a closed or partially open position   .

Recessed latch-operating devices that are accessible to people with disabilities are available.  Verify requirements of authorities having jurisdiction.

Latch and Keeper:  Manufacturer's standard recessed  latch unit designed for emergency access and with combination rubber-faced door strike and keeper.  Provide units that comply with regulatory requirements for accessibility at compartments designated as accessible.

Coat Hook:  Manufacturer's standard combination hook and rubber-tipped bumper, sized to prevent in-swinging door from hitting compartment-mounted accessories.

Door Bumper:  Manufacturer's standard rubber-tipped bumper at out-swinging doors.

Door Pull:  Manufacturer's standard unit at out-swinging doors that complies with regulatory requirements for accessibility.  Provide units on both sides of doors at compartments designated as accessible.

Retain first paragraph below for overhead-braced units.  Revise if specific finish is required.  Generally, clear-anodized finish is provided.

Overhead Bracing:  Manufacturer's standard continuous, extruded-aluminum head rail with antigrip profile and in manufacturer's standard finish.

Revise paragraph below to suit Project.

Anchorages and Fasteners:  Manufacturer's standard exposed fasteners of stainless steel to match the items they are securing, with theft-resistant-type heads.  Provide sex-type bolts for through-bolt applications.  For concealed anchors, use stainless steel fasteners.

FABRICATION

Retain applicable mounting styles in first four paragraphs below.

Overhead-Braced Units:  Provide manufacturer's standard corrosion-resistant supports, leveling mechanism, and anchors at pilasters to suit floor conditions.  Provide shoes at pilasters to conceal supports and leveling mechanism.

Urinal-Screen Posts:  Provide manufacturer's standard corrosion-resistant anchoring assemblies with leveling adjustment at bottoms of posts.  Provide shoes at posts to conceal anchorage.

Retain paragraph below and revise to suit Project if door sizes and swings are not shown on Drawings; verify requirements of authorities having jurisdiction.

Door Size and Swings:  Unless otherwise indicated, provide 24-inch- (610-mm-) wide, in-swinging doors for standard toilet compartments and 36-inch- (914-mm-) wide, out-swinging doors with a minimum 32-inch- (813-mm-) wide, clear opening for compartments designated as accessible.

EXECUTION

INSTALLATION

General:  Comply with manufacturer's written installation instructions.  Install units rigid, straight, level, and plumb.  Secure units in position with manufacturer's recommended anchoring devices.

Maximum Clearances:

Pilasters and Panels:  1/2 inch (13 mm).

Panels and Walls:  1 inch (25 mm).

Retain subparagraph below for stirrup brackets.  For solid-polymer units, three brackets are recommended for panel-to-wall and panel-to-pilaster connections to prevent sagging of panel.

Retain applicable mounting styles in first four paragraphs below.

Overhead-Braced Units:  Secure pilasters to floor and level, plumb, and tighten.  Set pilasters with anchors penetrating not less than 1-3/4 inches (44 mm) into structural floor unless otherwise indicated in manufacturer's written instructions.  Secure continuous head rail to each pilaster with no fewer than two fasteners.  Hang doors to align tops of doors with tops of panels, and adjust so tops of doors are parallel with overhead brace when doors are in closed position.

Urinal Screens:  Attach with anchoring devices to suit supporting structure.  Set units level and plumb, rigid, and secured to resist lateral impact.

ADJUSTING

Revise hinge adjustment requirements in this article to suit Project.  Verify accessibility requirements of authorities having jurisdiction.

Hardware Adjustment:  Adjust and lubricate hardware according to hardware manufacturer's written instructions for proper operation.  Set hinges on in-swinging doors to hold doors open approximately 30 degrees from closed position when unlatched.  Set hinges on out-swinging doors[ and doors in entrance screens] to return doors to fully closed position.

END OF SECTION 10 21 13